## Slide 1
13 мая 2021 г
Виктор Толстопятов
Инженер по применению силовых модулей
Новая линейка силовых Si и SiC транзисторных модулей в корпусах LV100, HV100 для тяговых применений

## Slide 2
Outline of HV Development
X series
(Si)
std
(standard)
6kVrms
10kVrms
Dual (RG)
（デュアル）
LV100
(6kVrms)
HV100
(10kVrms)
SiC
dual
dual
LV100
(6kVrms)
series | package | Viso | picture

## Slide 3
Point
◆ 7th gen. IGBT chip and RFC diode chip reduce power loss
◆ Industry-leading power density* for increased inverter capacity
◆ The terminal layout is optimized for easy paralleling and flexible inverter configurations and capacities
LV100 type
HV100 type
Internal circuit
LV100 type
HV100 type
LV100/HV100 Type
Notes: 40%改善

## Slide 4: X-series Dual type : LV100 / HV100
Type | LV100 |  | HV100 |  | 
Isolation | 6.0kV |  | 10.2kV |  | 
Rated voltage | 1.7 kV | 3.3 kV | 3.3 kV | 4.5kV | 6.5kV
Rated current | 1200A 900 A | 600A 450 A | 600A 450 A | 450A 350A | 300A 225A
Notes: 広報発表内容の事前通知と電源展とPCIM展示内容の紹介および推奨ドライバを準備中であることを伝える。

## Slide 5
Power density comparison of 3.3kV/600A
4.51 A/cm2
CM1200HC-66H
CM1500HC-66R
5.64 A/cm2
6.77 A/cm2
CM1800HC-66X
The highest current density in the industry is realized
CM600DC-66X
8.57 A/cm2
3.3kV
Notes: 40%改善

## Slide 6: Low inductance package
➤Very low internal inductance by laminated/symmetrical structure
Laminated terminal structure

## Slide 7: Low inductance package
Inductive switching
test setup
➤Safe turn-off possible at large current without snubber capacitor
1200A, 1700V module. Turn-off waveform
without snubber cap. @Tvj=25C, RG=0Ω
IC:400A/div
VCE:300V/div
VCEpeak=1690V
Turn-off Ic=2400A
time:200ns/div
VCC=1200V
No snubber capacitor
Notes: ・VCEモニタはセンス-センス
・N側波形。P側では1717Vをマーク。

## Slide 8
CM450DC-66X
CM600DC-66X
500A
1000A
1500A
2000A
2500A
Easy parallel connection
450A
900A
1350A
1800A
600A
1200A
1800A
2400A
3.3kV

## Slide 9: Example of bus bar Layout
Laminated Busbar
Gate Driver
HVIGBT LV100
Capacitor
DC side
AC side
AC side
DC side
Simple PCB layout and simple output line layout

## Slide 10: Optimized Layout
ideal module (terminal and chip arrangement is perpendicular to current flow)
AC
P
N
P
AC
AC
AC
P
X
Y
LV100 (based on ideal module concept)
P-side chips
N-side chips
Current direction (only Y)
Conventional Module (chips arrangement is parallel to current flow)
All chips have same impedance
All chips have almost same impedance
All chips have different impedance
N
P
AC
Current direction is mainly X
N
N

## Slide 11
Switching behavior in 4 parallel
IC_A
IC_B
VCE
VCE
Turn-on
Turn-off
 | di/dt [A/μs] | ICP [A] | Eon [J] | IC [A]
#A | 5133 | 1955 | 0.558 | 607
#B | 5163 | 1864 | 0.482 | 581
#C | 5709 | 1872 | 0.749 | 598
#D | 4271 | 1833 | 0.571 | 589
Δ/ave | 28.4 % | 6.5 % | 45.2 % | 4.4 %
 | di/dt [A/μs] | Eoff [J] | IC [A]
#A | 1672 | 1.12 | 592
#B | 1682 | 1.09 | 604
#C | 1622 | 1.00 | 588
#D | 1704 | 1.04 | 604
Δ/ave | 5.0% | 9.0% | 2.7%
IC_C
IC_D
IC_A
IC_B
IC_C
IC_D
Condition: VCC = 1800V, IC = 600A/module, Tj = 150℃
3.3kV/600A
Notes: 40%改善

## Slide 12
Technical advantages
Notes: 40%改善

## Slide 13
The new package structure for high reliability Tj
Notes: 40%改善

## Slide 14
Chip technologies
Inverter losses reduction
New trench gate structure
→ CSTBTTM (III)
Higher carrier concentration at emitter side under on-state
Lower VCEsat
CSTBTTM (III) (CSTBT: Carrier Stored Trench Gate Bipolar Transistor)
Wide SOA margin
→ Partial P collector
Minimize hole injection efficiency in edge termination
Partial P collector
Improvement output current & Rth
New edge termination structure
→ LNFLR(Linearly-Narrowed Field Limiting Ring)
+SCC (Surface Charge Control)
Active area is increased by shrinking edge termination area
Robustness against humidity
3.3kV IGBT
①CSTBTTM(Ⅲ)
③Partial P-Collector
②LNFLR + SCC
R-Series
X-Series
Notes: 40%改善

## Slide 15: Robustness against humidity (Surface Charge Control technology)
Conventional structure
X-series structure (SCC technology)
Surface charge due to humidity is discharged and therefore robustness against humidity is achieved.
Gel appearance
(foggy)
SCC (Surface Charge Control)
Condensation test result
(CM1000HG-130XA)
No ICES increase!

## Slide 16: Wide SOA margin
RBSOA & RRSOA Type test (CM1500HC-66R)
Conditions :
Tj = 150 C, VCC = 2500 V, IC = 6000 A, LS = 140 nH
Conditions :
Tj=150C, Vcc=2500V, di/dt & Ls= adjustable
RBSOA Type test
RRSOA Type test
Design target: 2 times higher than SOA
2 times
2 times

## Slide 17
Chart: Passive P/C curve @Tjmax=150°C, Ic=1800A
| 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
CM1500HC-66R P/C curve | 33371356 | 5303818 | 1227808 | 363962 | 128522 | 51701 | 23004 | 11091
CM1800HC-66X | 313773103.3514 | 85793920.808 | 28635083.7571 | 11059374.03 | 4775030.6412 | 2251161.3337 | 1139526.7919 | 611703.1185 | 344954.3632 | 202863.9471 | 123693.5315 | 77831.1286 | 50345.3402 | 33372.2579 | 22608.7517 | 15619.0365 | 10982.0517
Improved Power cycling lifetime:
More than 2 times improved new X-Series design

## Slide 18
 | carrier | Blocking voltage | SW loss | territory
MOSFET | Electron (unipolar) |  |  | < 600V
IGBT | Electron + Hole (bipolar) |  |  | > 600V
 |  | MOSFET | IGBT
Blocking voltage (V) | Thickness of n- layer (um) | VDS(on) (V) | VCEsat (V)
600 | 50 | 1.6 | 1.6
1200 | 100 | 9.0 | 1.8
1700 | 140 | 21.5 | 2.0
ON state voltage comparison MOSFET vs IGBT on Si base
Benefit of SiC power device
ON state voltage of IGBT is reduced
by conductivity modulation

## Slide 19
material | Breakdown strength (V / um )
4H-SiC | 300
Si | 30
p
n+
n+
source
n-
drain
1200V Si-MOSFET
≒100µm
RDRIFT
p
n+
n+
source
n-
drain
1200V SiC-MOSFET
≒10µm
ON state voltage
Si >> SiC
10 times higher
breakdown strength than Si

## Slide 20
Type | Product | Model | Specification | Dimensions
LV100 (6kViso) | SiC hybrid module | CMH1200DA-34X | 1.7kV/1200A/2in1 | 100×140×40mm3
 |  | CMH600DA-66X | 3.3kV/600A/2in1 | 
LV100 Hybrid SiC modules
SiC-SBD

## Slide 21
LV100 3.3kV Full SiC module
Type | Product | Model | Specification | Dimensions
LV100 (6kViso) | Full-SiC module | FMF750DC-66A | 3.3kV/750A/2in1 | 100×140×40mm3

## Slide 22
Inverter loss Comparison
condition:
VCC = 1800V, IO = 450Apeak, fc = 5kHz, P.F.=0.85, M=1
Chart: Inverter losses [W]
| CM600DA-66X | CMH600DA-66X | FMF750DC-66A
DC(IGBT) | 272.7864 | 272.7864 | 212.1669
SW(on) | 1072.3111 | 536.1556 | 395.6719
SW(off) | 1302.0781 | 1302.0781 | 180.5995
DC(diode) | 43.3134 | 57.5407 | 54.4558
SW(rec) | 1329.975 | 38.4303 | 46.1442
-76%
Hybrid SiC
Full SiC
Si IGBT
-45%

## Slide 23
Requirement from Rail Car market
to save energy
to fully utilize limited underfloor space, smaller inverter is desirable
Propulsion Inverter
Full-SiC power module
SiC
MOS
SiC-SBD
Limited space
SiC Merits in railway application

## Slide 24
Running Resistance 47%
Gear 6%
Filter loss 11%
Mechanical brake 15%
Motor loss 17%
Invertor 2%
Others 2%
Energy loss share of Propulsion Inverter
Invertor loss is not majority
Save energy in smaller space
focus on these two points
SiC Merits in railway application

## Slide 25
wave form with conventional invertor
wave form with high switching SiC invertor
Motor loss improvement
Current
voltage
Ideal sine wave
Current
voltage
Ideal sine wave
harmonic loss reduction
Motor harmonic loss can be reduced on smaller cooling fin
by SiC power module
Current distortion
SiC Merits in railway application

## Slide 26
Regenerative brake power can be expanded on smaller
cooling fin by SiC power module
Mechanical loss improvement  Regenerative brake area expansion
speed
Brake power
high
0
speed
Brake power
high
0
Conventional brake system
Developed brake system
Mechanical brake
Regenerative brake
Mechanical brake
Regenerative brake
Regeneration brake power is expanded
Regenerative brake can return kinetic energy to catenary
Synchronous
rectification
SW
device
diode
SiC Merits in railway application

## Slide 27
motor harmonic loss
reduction
Conventional
inverter
Full-SiC
inverter
Regenerative power expansion
Energy consumption
comparison
Results on SiC power module
Save energy on smaller size was realized
SiC Merits in railway application

## Slide 28
Auxiliary power supply circuit example
リーケージトランス又はリアクトル
volume share of Auxiliary power supply
Volume share of AC filter and invertor are more than 50%
cooling fin kept smaller due to power loss reduction by SiC power module.
AC filter size kept smaller due to higher fc by SiC power modules.
capacitor
AC filter
invertor
AC out
Trans former
Filter
reactor
breaker
AC filter
invertor
Filter
reactor
capacitor
others
breaker
Auxiliary power supply
Save energy in smaller space
Notes: 箱内に収める部品が、走行用インバータ装置と異なる。巻物を箱内に抱いている。
＜語順注意＞
スイッチングリプルを負荷側に漏えいさせないためのフィルタ用のＡＣリアクトルがポイント。
変圧（絶縁）機能のためのトランスの、漏れインダクタンスで代用できるくらいに高周波化するとインパクト。 「又は」⇒「および」

## Slide 29
●size : 20% down & weight : 15% down
●energy saving : total loss reduce 30%
●noise reduction -4dB
Out put : AC 200V 60Hz
Output power：140kVA
Cooling：air cooling
Power supply
Results of Auxiliary power supply
Cooling fin of inverter was kept smaller due to power loss reduction
by SiC power module.
AC filter size kept smaller due to higher fc by SiC power modules.
To Save energy in smaller space is realized by SiC module
Save energy in smaller space
Notes: EMCも改善可能か
●TMK1000に納入した添付のSiC補助電源:2280Hz(同案件Si装置:1620Hz)
·その他SiC補助電源:2340Hz、3060Hz、4500Hz、5.5kHzなど
·一般的なこれまでのSiの補助電源装置:1950Hz、2340Hz
●他社さんから、full-SiCで、高周波リンクタイプのご提案あり。
今後、高周波タイプへの対応も広がる。リアクトル等の選定、最適化が課題

## Slide 30
1.7kV SiC Hybrid Module for Traction Application

## Slide 31: END
Виктор Толстопятов
victor.tolstopyatov@mer.mee.com
Phone/WhatsApp: +7-985-490-26-03